BFGRP – BaseZone® Flat Guard Rail Post Padding
SECTION 11 68 33
Athletic Field Equipment
(Formerly Section 11480)

PART 1
GENERAL 
1.01

WORK INCLUDED

A.

Provide all equipment and materials, and do all work necessary to furnish 



and install the athletic equipment, as indicated on the drawings and as 



specified herein.  Athletic equipment shall include, but not be limited to:

1. BFGRP – BaseZone® Flat Guard Rail Post Padding 
1.02

RELATED WORK

A.

Examine contract documents for requirements that affect work of this 



section.  Other specification divisions and sections that directly relate to
                       
the work of this section include, but are not limited to:




1.  Division 03 – Concrete; Sections: Cast-in-Place Concrete 

2.  Division 31 – Earthwork; Sections: Excavation and Backfill and
                                        Establishment of Sub-Grade Elevations




3.  Division 32 – Exterior Improvements; Sections: Athletic and





    Recreational Surfacing, Concrete, Asphalt and
                                                                Site Improvements 
1.03

REFERENCES

A.

Comply with applicable requirements of the following standards.  Where 



these standards conflict with other specified requirements, the most 



restrictive requirements shall govern.
1.  National Federation of State High School Associations (NFHS)




2.  National Collegiate Athletic Association (NCAA)





3.  Minor League Baseball (MiLB)





4.  Major League Baseball (MLB)




5.  International Association of Athletics Federations (IAAF)




6.  ASTM International


7.  American Sports Builders Association (ASBA)



8.  Manufacturers Data and Recommended Installation 




     Requirements

1.04

SUBMITTALS

A.

Manufacturers Product Data




1.  Provide manufacturers product data prior to actual field 




     installation work, for Architects or Owners representatives 




     review.

B.

Shop Drawings




1.  Provide drawings of the manufacturers recommended 




     installation and foundation requirements prior to actual field 




     installation work, for Architects or Owners representatives 




     review.

1.05

QUALITY ASSURANCE

A.

Manufacturers warranties shall pass to the Owner and certification made 



that the product materials meet all applicable grade trademarks or conform 

to industry standards and inspection requirements.

1.06

PRODUCT DELIVERY AND STORAGE

A.

Materials delivered to the site shall be examined for damage or defects in 


shipping. Any defects shall be noted and reported to the Owners 



representative. Replacements, if necessary, shall be immediately re-


ordered, so as to minimize any conflict with the construction schedule.  


Sound materials shall be stored above ground under protective cover or 


indoors so as to provide proper protection.
PART 2
PRODUCTS 
2.01

BFGRP – BaseZone® Flat Guard Rail Post Padding
A. 
BASE: BFGRP – BaseZone® Flat Guard Rail Post Padding as Manufactured and/or Supplied by:
Sportsfield Specialties, Inc.  

P.O. Box 231 

41155 State Highway 10





Delhi, NY 13753   

p. 888-975-3343

f. 607-746-8481

www.sportsfield.com
B.

COMPONENTS:  
1. BFGRP – BaseZone® Flat Guard Rail Post Padding:
a. Dimensions: 6”W x Variable Length x 2” Thick
b. Premium Outdoor Vinyl Encasement:

i. High UV Resistance

ii. Total Weight: 19 oz./yd2 (ASTM D3776)

iii. Construction: 18 x 18, 1300 x 1300 Denier

iv. Grab Tensile: Warp 750 lb/2”, Fill 655 lb/2”. (ASTM D5034)

v. Tongue Tear: Warp 153 lb/in., Fill 135 lb/in (ASTM D2261)

vi. Adhesion: 38 lb/2” (ASTM D571)

vii. Cold Crack: -30° F (ASTM D2136)

viii. Rot, Mildew and Fungus Resistant: Yes

ix. Various Standard Colors Available

c. 1.25” Thick High Density Polyethylene Cross-Link Closed Cell Foam
i. Density: 1.7 pcf

ii. Tensile Strength: 20 psi

iii. Elongation: 95%

iv. Tear Resistance: 7 lb/in

v. Compression Strength:

1. @ 25% psi: 4 psi

2. @ 50% psi: 7 psi

vi. Compression Set: 29% of Original Thickness

vii. Thermal Stability: < 0.5% of Change @ 158°F for 22 hrs

viii. Thermal Conductivity: 0.20 btu/hr/inch ft/ׄ°F

ix. Working Temperature Range: -70 °F to 175 °F

x. Water Absorption: <0.06 lb/ft2/°F

xi. Flammability: Pass (MVSS302)
d. 3/4” Square Edge AdvanTech® Water Resistant Sheathing Panel, All Sides Stained and Sealed with Exterior Grade Finish
e. Includes Galvanized and/or Stainless Steel Attachment Hardware to Fit the Applicable Rail Size(s)
f. 1-Year Manufacturer’s Limited Product Warranty

g. Optional

i. Custom High-Resolution Digitally Printed Graphics
PART 3 
EXECUTION

3.01

INSTALLATION OF EQUIPMENT

A.  
All BFGRP – BaseZone® Flat Guard Rail Post Padding shall be installed as recommended per manufacturer's written instructions and as indicated on the drawings.  Installer should have a minimum of five (5) protective padding installations or similar experience in the previous three (3) years.  
    
END OF SECTION
Athletic Field Equipment
11 68 33
12.20.24

